3838 Conductive Metallisation导电喷涂金属粉

Conductive metallisation 3838导电喷涂金属粉

For higher demands and larger quantities we can sputter a full metal coating on 90% of all commonly used plastics, even on PTFE! Applied as a sandwich of three thin layers of metal.

对于更高要求和大量的使用我们能喷射一个完全金属涂层在90%的所有通常使用的塑料制品上，即使在PTFE上！应用作为一个三个金属薄层的三明治。

First a thin layer of stainless steel, to prevent the softeners in the plastic affecting the shielding. Secondly a thin layer of copper for superb shielding performance. And thirdly another layer of stainless steel to avoid corrosion.

第一个薄层是不锈钢的，用于防止软化剂在塑料里影响屏蔽。第二个薄层是铜的，用于杰出的屏蔽效能。第三个薄层是不锈钢的，用于规避腐蚀。

Shielding performance屏蔽性能

| Frequency (Mhz)频率 | Metallisation (dB)喷涂金属粉 |
| --- | --- |
| 30 | 50 |
| 100 | 58 |
| 200 | 70 |
| 500 | 74 |
| 700 | 72 |
| 900 | 70 |
| See Guarantee |  |