1200 Metal knit gasket金属编织垫圈

Knitted Mesh is a Universal EMC gaskets to shield lower frequencies编织网是一个通用的EMC垫圈以屏蔽较低的频率。

For permanent or fixed panel mating surfaces.用于永久的或固定的面板接触面。

The 1200 metal knit gasket serie EMC gaskets consist of a layer of knitted metal wires over a low-closure-force rubber or elastomer core. For applications like EMP or high temperatures a full metal version is available. Metal knit gasket is sometimes combined with an environmental seal to provide IP rating, depending on the materials used.

该1200金属编织垫圈系列EMC垫圈由在一个低闭合力橡胶或弹性体核上面有一层编织金属线组成。对于应用如EMP或高温，可获得一个全金属版本。金属编织垫圈有时与一个环境密封结合以提供IP等级，依据使用的材料。

The temperature resistance depends on the core material of the metal knit gasket, but ranges from -60°C to 220°C are possible. These metal knit gaskets are insensitive to external influences and can withstand harsh conditions very well.

耐温性依据金属编织垫圈的核材料，但范围从-60°C to 220°C是可能的。这些金属编织垫圈是不易感受外部影响的，能非常好的承受严厉的条件。

The maximum deflection with a sponge elastomer core is approximately 30%, with hollow extrusion 50%. This is why the hollow type is used more often.

最大挠度用海绵弹性体核的大约是30%，用空心弹性体的是50%。这是为什么空心类型的通常使用的更多的原因。

For high frequency shielding, foil-based gaskets like Amucor Shield 6800 will perform better, because of their much larger contact surface. Please take a look at the image below to understand.

对于高频屏蔽，基于薄片的的垫圈如Amucor Shield 6800将执行的更好，因为它们有跟大的接触面。请注视下列的图形可明白。

Advantages优势:

- High attenuation level for lower frequencies; 对于低频有高的衰减级别。

- Suitable for use under extreme conditions (military applications) 适合于使用在最恶劣的条件下（军事应用）

- Wear resistant; 耐磨

- Insensitive for corrosion;耐腐蚀

Technical specifications技术规格

| Material材料 | Applications应用 |
| --- | --- |
| Monel蒙乃尔铜-镍合金 Per QQ-N-281 BS 3075 N A 13 Class A diameter直径 0.11mm | The most common used material.最普遍使用的材料 Insensitive to corrosion and neutral on the galvanic scale.不受腐蚀的影响及是中性的在电化氧化方面。 |
| Aluminium铝 AMS 4187 BS 1475 5056A Alloy 合金5056 diameter 直径0.13mm | Is used in some cases for aluminium enclosures.用于铝外壳的一些情况。 Aluminium can be chromated with an Alchrome 1200 layer, if necessary. |
| T.C.S. Steel Core钢心(57%) Copper cladding铜镀层(40%) Tin Plating镀锌板 (3%) diameter直径 0.11mm | This material has excellent magnetic as well as electrical properties, because a Ferro alloy is covered with copper.这个材料有卓越的磁和电特性，因为一个一个亚铁合金被用铜覆着。 The outside is tinned to prevent corrosion. 外部是镀锡的以预防腐蚀。 |
| Stainless steel不锈钢 AISI 304 diameter直径 0.13mm | The strongest material with a shielding performance that can be compared with aluminium. High resistance against wear.最强的屏蔽性能的材料与铝相比。高的耐磨性。 |

Shielding performance屏蔽性能

| Frequency频率 | Field场 | Monel蒙乃尔铜镍合金 | Aluminium铝 | TCS | S/Steel不锈钢 |
| --- | --- | --- | --- | --- | --- |
| 10 KHz | H | 45 | 40 | 60 | 40 |
| 100 KHz | H | 49 | 45 | 65 | 44 |
| 1 MHz | H | 60 | 60 | 85 | 58 |
| 1 MHz | E | 125 | 125 | 125 | 125 |
| 10 MHz | E | 120 | 120 | 120 | 120 |
| 100 MHz | E | 100 | 100 | 108 | 100 |
| 400 MHz | P | 98 | 95 | 99 | 94 |
| 1 GHz | P | 85 | 76 | 78 | 76 |
| 10 GHz | P | 80 | 65 | 62 | 60 |

Stock dimensions存储尺寸

| Fully metal round (R)完全的金属环. D (mm). 1.6. 2.4. 3.2. 4.0. 4.8. 6.4. 7.9. 9.5. 11.1. 12.7. |  | Hollow round (HR)空心环. D x d (mm). 3.2 x 1.6. 4.8 x 3.2. 6.4 x 3.2. 8.0 x 4.8. 9.5 x 6.4. 11.1 x 8.0. 12.7 x 9.5. 14.9 x 11.1. |  |
| --- | --- | --- | --- |
| Double fully metal round (B)双全金属环. d x w (mm). 1.6 x 9.5. 1.6 x 12.7. 1.6 x 15.9. 2.4 x 12.7. 3.2 x 9.5. 3.2 x 12.7. 3.2 x 15.9. 4.8 x 15.9. 4.8 x 19.1. 4.8 x 25.4. 6.4 x 15.9. 6.4 x 19.1. 6.4 x 25.4. 12.7 x 25.4. |  | Double hollow round (HB)双空心环. d x w (mm). 3.2 x 9.5. 3.2 x 12.7. 3.2 x 15.9. 4.8 x 15.9. 4.8 x 19.1. 4.8 x 25.4. 6.4 x 15.9. 6.4 x 19.1. 6.4 x 25.4. 9.5 x 25.4. 12.7 x 25.4. |  |
| Fully metal round with tail (T)全金属环带有尾巴. d x w (mm). 1.6 x 9.5. 1.6 x 12.7. 1.6 x 15.9. 2.4 x 12.7. 2.4 x 15.9. 3.2 x 12.7. 3.2 x 15.9. 3.2 x 19.1. 4.0 x 12.7. 4.0 x 19.1. 4.8 x 15.9. 4.8 x 19.1. 4.8 x 25.4. 6.4 x 15.9. 6.4 x 19.1. 6.4 x 25.4. 7.9 x 15.9. 7.9 x 19.1. 7.9 x 25.4. 9.5 x 15.9. 9.5 x 19.1. 9.5 x 25.4. 11.1 x 19.1. 11.1 x 25.4. 12.7 x 19.1. 12.7 x 25.4. |  | Hollow round with tail (HT)空心环带有尾巴. d x w (mm). 1.6 x 12.7. 1.6 x 15.9. 1.6 x 19.1. 2.4 x 12.7. 2.4 x 19.1. 3.2 x 12.7. 3.2 x 16.0. 3.2 x 19.1. 4.0 x 12.7. 4.0 x 19.1. 4.8 x 12.7. 4.8 x 15.9. 4.8 x 25.4. 6.4 x 12.7. 6.4 x 15.9. 6.4 x 19.1. 6.4 x 25.4. 9.4 x 19.1. 9.4 x 25.4. |  |
| Full metal rectangular (S) 全金属矩形. w x h (mm). 3.2 x 1.6. 3.2 x 3.2. 3.2 x 4.0. 3.2 x 4.8. 3.2 x 6.4. 4.8 x 4.8. 6.4 x 1.6. 6.4 x 3.2. 6.4 x 6.4. 9.5 x 6.4. 12.7 x 6.4. 12.7 x 9.5. 12.7 x 12.7. 15 x 6. 15 x 8. 15 x 10. 15 x 12. 15 x 15. 15.9 x 9.5. 19.1 x 12.7. 20 x 6. 20 x 8. 20 x 10. 20 x 12. 20 x 20. 25 x 6. 25 x 8. 25 x 10. 25 x 12. 25 x 18. 25 x 20. |  | Hollow rectangular (HS) 空心矩形. w x h (mm). 2.4 x 3.2. 2.4 x 4.8. 2.4 x 6.4. 3.2 x 3.2. 3.2 x 4.8. 3.2 x 6.4. 3.2 x 9.5. 4.8 x 4.8. 4.8 x 6.4. 4.8 x 9.5. 6.4 x 6.4. 6.4 x 9.5. 6.4 x 12.7. |  |

All knitted mesh gaskets can be produced with water seal.所有的编织网垫圈能被扩展水封。

Example举例

1200 Series metal knit gasket, neoprene core with monel cover, hollow rectangular shape, 3.2 x 1.6 mm with standard 10 mm width waterseal

1200系列金属编织垫圈，氯丁橡胶核带有蒙乃尔合金覆着，空心矩形形状，3.2 x 1.6 mm带有标准的10mm宽度水封。

| Serie系列 | Core核心 | Material材料 | Shape形状 | Dimensions尺寸 | Waterseal水封 | Width宽度 (mm) |
| --- | --- | --- | --- | --- | --- | --- |
| 1200 | C | M | HS | 3.2 x 1.6 | S | 10 |
|  | N : Not important不重要 F : Full metal全金属 H : Hollow silicone空心硅树脂 C : Neoprene氯丁橡胶 S : Sillicone硅树脂 E : EPDM三元乙丙橡胶 O : Hollow空心 | N : Not important不重要 M: Monel蒙乃尔铜镍合金 T : TCS A : Alluminium铝 S : Stainless stell不锈钢 E : Steel钢 | R : Fully metal round全金属环 HR : Hollow round空心环 B : Double fully metal round双全金属环 HB : Double hollow round双空心环 T : Fully metal round & tail全金属环带尾巴 HT : Hollow round & tail空心环带尾巴 S : Fully metal rectangular全金属矩形 HS : Hollow ractangular空心矩形 | Give the dimension from the dimension table 从尺寸表中给出尺寸 | S : Standard waterseal标准水封 P : Soft "P" seal软的密封 N : No waterseal没有水封 | Specify the width of the waterseal in mm 用毫米单位指定水封宽度 |