7000 Standard Shield标准屏蔽垫圈

For panels and screwed applications用于面板和螺丝拧紧的应用

Standard shield标准屏蔽垫圈

7000 series系列

Standard Shield 7000 is an economical HF gasket which can be supplied in a wide range of dimensions. It is very effective in combination with stainless steel, copper and chrome-plated constructions.

标准屏蔽7000是一个经济的HF垫圈，供货可以有一个宽的尺寸范围。它是非常有效的与不锈钢、铜和镀铬板结构的结合。

All gaskets can be provided with a (conductive) self-adhesive strip.

所有垫圈能供应一个(导电)自粘条。

Standard Shield 7000 consists of a neoprene or PVC foam core covered with textile. This guarantees excellent shielding performance and it is very strong.

标准屏蔽7000由一个氯丁橡胶或PVC泡沫核覆着织物组成。这个确保卓越的屏蔽性能和它是非常强壮的。

For special applications, different foam cores, conductive foils and fabrics are available.

对于特殊的应用，不同的泡沫核，导电箔和织物可获得。

Shielding Performance屏蔽性能

Shielding effectiveness depends on surface, shape of gaskets and material used. 屏蔽效能依据垫圈的表面、形状和使用的材料。

| Frequency Hz频率 | Mode | Screening屏蔽 dB |
| --- | --- | --- |
| 1M | E | 115 |
| 10M | E | 108 |
| 100M | E | 102 |
| 400M | E | 92 |
| 1G | P | 90 |
| 10G | P | 87 |
| See Guarantee |  |  |

Benefits好处

- Self-adhesive EMC gasket 自粘的EMC垫圈

- Easy to fit, can be cut with scissors 容易装配，能用剪刀剪切

- Good water resistance 好的耐水性

- Gasket can be die-cut (screwholes) 垫圈能被冲切（螺丝孔）

- Roll lengths up to 50, 100, 250 or 1000 m 一卷的长度可达50,100,250或1000米

- High shielding performance 高的屏蔽性能

- Low closure force 低的闭合力

- EXTREMELY STRONG 非常强壮的

- Deflection挠度50%

Options选件

- Cut into specific lengths 剪切成为指定的长度

- Can be made die cut or frame 能被冲切或加框

- Combination with water seal 兼具水封

- UL94V-0 flame retardant foam core 阻燃剂泡沫核

- Chemical resistant rubbers like EPDM 耐化学橡胶，如EPDM三元乙丙橡胶

- Silicone sponge for high temperatures up to 220°C 硅树脂海绵用于高温可达220°C

- Different conductive foils and fabrics 不同的导电箔和织物

Specifications规格说明

Foam core: Open-celled neoprene foam

泡沫核：开室的氯丁橡胶泡沫

Surface resistance: <0.08 square ohms

表面阻抗：<0.08 square ohms

Surface material: Conductive fabric (Polyester + Cu, Ni) (part no. 4711)

表面材料：导电织物(聚酯纤维+ Cu, Ni) (零件号. 4711)

Operating temperature运行温度: - 20°C / + 80°C

Environmental环境: RoHS Compliant

Adhesive specifications黏合剂规格

(Standard type标准类型)

Our adhesive is a transparent double-sided tape consisting of a PP-film backing and a tackified acrylic adhesive.

我们的黏合剂是一个透明双面带，由一个PP-薄膜背面和一个有黏性的丙稀酸黏合剂组成。

Backing material背面材料: PP film薄膜

Color颜色: Transparent透明

Thickness of tape条的厚度: 100 μm

Type of adhesive黏合剂类型: Tackified acrylic有黏性的丙烯酸

Elongation at break断裂伸长率: 140 %

Tensile strength拉伸强度: 20 N/cm

Type of line线型: MOPP

Thickness of liner线的厚度: 80 μm

Adhesion to steel铁的粘合: (after 14 days) 13,7 N/cm

Adhesion to PET的粘合: (after 14 days) 8,5 N/cm

Core specifications核的规格说明

(Standard Neoprene foam标准氯丁橡胶泡沫)

- Hardness shore 00硬度 : 38-55 Sh 00

- Resistance when compressed压阻 : 25% 350-630 g/cm2

- Temperature °C温度 (continuous连续的) : - 40°C / + 85°C

- Temperature °C 温度(peak峰值) : 100°C

- Max. deformation最大值变形 (compressed压缩) : 25% for 22 hrs at 70°C : 12%

- Recommended max. compression推荐的最大值压缩 : 25%

- Resistance to cold耐寒性 : Good好

- Resistance to air and ozone耐空气和臭氧 : Good好

- Resistance to mineral oils耐矿物油 : Good好

- Resistance to vegetable oils耐植物油 : Good好

- Resistance to acids耐酸 : Good好

- Resistance to chlorine solutions耐氯溶液 : Good好

- Flame retardancy阻燃性: Self extinguishing自熄灭

Mechanical proporties机械特性

Standard dimensions标准尺寸

Dimensions尺寸

| Width X(mm)宽度 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Height高度 Y(mm) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 12 | 15 | 18 | 20 | 25 | 32 | 50 |  |  |
|  | 1 | 7021 | 7031 | 7041 | 7051 | 7061 | 7071 | 7081 | 7091 | 70101 | 70121 | 70151 | 70181 | 70201 | 70251 | 70321 | 70501 |  |  |
|  | 2 | 7022 | 7032 | 7042 | 7052 | 7062 | 7072 | 7082 | 7092 | 70102 | 70122 | 70152 | 70182 | 70202 | 70252 | 70322 | 70502 |  |  |
|  | 3 |  | 7033 | 7043 | 7053 | 7063 | 7073 | 7083 | 7093 | 70103 | 70123 | 70153 | 70183 | 70203 | 70253 | 70323 | 70503 |  |  |
|  | 4 |  |  | 7044 | 7054 | 7064 | 7074 | 7084 | 7094 | 70104 | 70124 | 70154 | 70184 | 70204 | 70254 | 70324 | 70504 |  |  |
|  | 5 |  |  |  | 7055 | 7065 | 7075 | 7085 | 7095 | 70105 | 70125 | 70155 | 70185 | 70205 | 70255 | 70325 | 70505 |  |  |
|  | 6 |  |  |  |  | 7066 | 7076 | 7086 | 7096 | 70106 | 70126 | 70156 | 70186 | 70206 | 70256 | 70326 | 70506 |  |  |
|  | 8 |  |  |  |  |  | 7078 | 7088 | 7098 | 70108 | 70128 | 70158 | 70188 | 70208 | 70258 | 70328 | 70508 |  |  |
|  | 9 |  |  |  |  |  |  |  | 7099 | 70109 | 70129 | 70159 | 70189 | 70209 | 70259 | 70329 | 70509 |  |  |
|  | 10 |  |  |  |  |  |  |  |  | 701010 | 701210 | 701510 | 701810 | 702010 | 702510 | 703210 | 705010 |  |  |
|  | 12 |  |  |  |  |  |  |  |  |  | 701212 | 701512 | 701812 | 702012 | 702512 | 703212 | 705012 |  |  |

Item numbers in bold are 98% stock items. Other dimensions on request.

项目号用黑色表示的是98%为存货项目。其它的尺寸根据需求。

Special shapes特殊形状:

| EPDM rubber | 700072 | 700068 | 700058 | 700064 | 700076 | 700051 |
| --- | --- | --- | --- | --- | --- | --- |
| Y x X mm | 2 x 4 mm | 3 x 6 mm | 4 x 8 mm | 8 x 12 mm | 10 x 12 mm | 16 x 20 mm |
| Y x X inch | .079" x .157" | .118" x .236" | .157" x .315" | .315" x .472" | .394" x .472" | 16 x 20 mm |

Tape Specification条的规格

01 : Standard self-adhesive placed in the middle 标准自粘布置在中间

02 : Without self-adhesive 不带有自粘

03 : With conductive self-adhesive 带有导电自粘

(only recommended on small sizes仅仅推荐在小尺寸上)

06 : Standard self-adhesive, asymmetrica标准自粘，非对称的

07 : Standard self-adhesive placed on the side 标准自粘布置在侧边上

Foam Specification泡沫规格

N : Standard Neoprene Foam标准氯丁橡胶泡沫

E : EPDM foam core 三元乙丙橡胶泡沫核

P : low closure force PVC Foam, slow recovery 低闭合力PVC泡沫，慢复原

F : Flame retardant Foam 阻燃剂泡沫(UL94V-0)

Datasheet数据表

| Page 1 (Standard shield标准屏蔽) | Page 2 (Neoprene foam core氯丁橡胶泡沫核) | Page 3 (Adhesive黏合剂) | Page 4 (EPDM foam core三元乙丙橡胶泡沫核) |
| --- | --- | --- | --- |

Example举例

Standard Shield 7000, 8 x 2 mm, standard self-adhesive placed in the middle, standard neoprene foam core: 7082-01-N

标准屏蔽7000，8 x 2 mm，标准自粘布置在中间，标准氯丁橡胶 ：7082-01-N

| Part number零件号 | Tape code条编码 | Foam code泡沫编码 |
| --- | --- | --- |
| 7082 | 01 | N |
|  | 01: standard self-adhesive placed in the middle标准自粘布置在中间 02: without self-adhesive 不带有自粘 03: with conductive self-adhesive (only recommended on small sizes)带有导电自粘（仅推荐在小尺寸上） 06 : standard self-adhesive, asymmetrical标准自粘，非对称的 07 : standard self-adhesive placed on the side标准自粘布置在侧边 | N : standard neoprene foam标准氯丁橡胶泡沫 E : EPDM foam core 三元乙丙橡胶泡沫核 P : low closure force PVC foam, slow recovery低闭合力PVC泡沫，慢复原 F : flame retardant UL94V-0 foam阻燃剂泡沫 |